# Ternary EuMg5+x-type structures: Challenges in refining channel occupancies
## M. Otteny, K. Köhler, M. Wendorff, C. Röhr
### Institut für Anorganische und Analytische Chemie, Albert-Ludwigs-Universität Freiburg
### markus.otteny@ac.uni-freiburg.de
The synthesis of polar intermetallic compounds and their structural chemistry is a key focus of our research. For the composition of approximately 1:5, the EuMg5+x structure type, besides the very common CaCu5-type, also occurs quite frequently. As indicated by the "x" in the eponymous compound, the exact number of atoms in the unit cell can vary [1], leading to challenges in structure refinement. In this work, we provide a summary of our findings on this structure type, based on studies of the ternary systems A–M–M’ (A = Ca, Sr, Ba; M = Mg, Zn; M’ = Zn, Cd, In) [2].
In the EuMg5+x-type structure of Ba3Mg5.2Cd10.8 (P63/mmc, a=1023.10(5), c=1082.63(5) pm), the A atoms are arranged in rings of three, filling the voids within a topologically close-packed (t.c.p.) network of M atoms. The latter network is formed by vertex-sharing double tetrahedral stars (Fig. 1, red) leaving empty channels along [001]. The electron density distribution within these channels, which varies from compound to compound and even along an M:M’ phase width [e.g. in Ca(MgyZn1-y)5+x (y = 0.1 - 0.9)], gives rise to many questions regarding the atomic distribution and it's crystal-chemical interpretation [3].
We describe the channels as strings of corner connected cubes. These cubes are also part of the M network. In the investigated systems the filling of these cubes varies leading to different models for the overall structure. For Zn containing compounds Zn2 dumbbells can be observed. In the Sr–Mg–In system additional reflexes can be observed which could be indexed with a rhombohedral unit cell
(P63/mmc → P31c → R3c, a = 1775.97(8), c = 3181.12(13) pm, Fig. 1). In this superstructure every third ‘cube’ is empty and heavily squeezed (Fig. 1, aquamarine), resembling less a cube and more a cluster consisting of six tetrahedra which share a common edge. Therewith, this structure motif fits the t.c.p. principle again.

###### Figure 1. Structure of Sr3Mg12.5In3.1, a superstructure of the EuMg5+x-type.

#### [1] Mühlpfordt, W. (1997) Z. Anorg. Allg. Chem. 623, 985-989.
#### [2] Köhler, K. (2022) PhD thesis, University of Freiburg; K. Köhler, C. Röhr. (2019) Acta Cryst. A75, 424.
#### [3] Fredrickson, R. T., Fredrickson, D. C. (2023). Acta Cryst. B79, 320-329.