# Heterobimetallic Mn(II)/Al(III) chalcogenides: Model systems for mixed-valent ferrates(II/III)
## C. Röhr1, M. Schwarz1
### 1Institut für Anorganische und Analytische Chemie, Universität Freiburg, Germany.
### Email: caroline@ruby.chemie.uni-freiburg.de
The heterobimetallic Mn/In [1] and Mn/Al (this work) metallates A3MnAlQ4 (A=K, Rb, Cs; Q=S, Se, Te) are model systems for the mixed-valent ferrates(II/III), where the M(II):M(III) ratio can be specifically adjusted during synthesis. While the pure p-block metallates(III) AAlIIIQ2 are dominated by layered structures of T2 supertetrahedra (KInS2-type 22, i.e., pure corner connections). Both the ferrates(III) AFeIIIQ2 and the manganates(II) A2MnIIQ2 exhibit linear chains of trans-edge-sharing [MQ4/2] tetrahedra KFeS2- 3 and K2ZnO2-type 1, respectively). In contrast, the mixed-valent salts AxMQ2, x=1-2), show a remarkably diverse crystal chemistry, which in the case of ferrates is accompanied by interesting magnetic properties: The entire series of of the hetero-bimetallic Mn(II):(Al/In)(III)=1:1 model systems A3[MnInQ4] (A=K-Cs, Q=S-Te, [1]) and A3[MnAlQ4] (A=K, Rb; Q=S-Te, this work, e.g. K3[MnAlS4]: orthorhombic, Pnma, a=716.5(3), b=1144.3(4), c=1147.5(2) pm, R1=5.06 %), which were obtained from stoichiometric melts, are isotypic to the analogous mixed-valent ferrates of the general composition A3Fe2S4 7 [2,3]. All of these compounds contain strongly corrugated tetrahedral chains, whereby - in the case of the Mn/Al and Mn/In compounds - the tetrahedra centers are statistically occupied by the two metal cations. Attempts to synthesize the analogous cesium Mn/Al metallates were unsuccessful, but in the case of sulfur they yielded the new orthorhombic compound Cs13Mn4Al5S18 (x=1.44, 9, Ima2, a=5270.7(5), b=1238.2(1), c=769.9(1) pm, R1=6.08 %) in virtually pure phase. With its complicated bent chains (running along the long a axis), this salt represents a model system for those mixed-valent ferrates in which the Fe(II):Fe(III) ratio deviates from 1:1 and which correspondingly exhibit large translation periods along the chains 10,11 [4], up to modulated structures e.g. in K7.15[FeS2]4 12 [5]. These similarities between the mixed-valent ferrates and the heterobimetallic Mn/Al and Mn/In metallates show, that only the 'odd' number of A+ counterions and by no means magnetic effects are responsible for the corrugation of the chains. Until now, 'tetrahedra stars' [M4Q8], which serve as model systems for the biologically relevant 4Fe4S clusters, are only observed in mixed-valence ferrates A6-7[Fe4Q8] 15-17 with Fe(II):Fe(III) ratios between 1:1 and 3:1 (x=1.5-1.75) [6].
[1] M. Langenmaier, J. Brantl, C. Röhr, J. Solid State Chem., 292, 121455 (2020).
[2] K. Klepp, H. Boller, Monatsh. Chem., 112, 83-89 (1981); K. Klepp, W. Sparlinek, Z. Kristallogr. NCS, 211, 626 (1996).
[3] W. Bronger, U. Ruschewitz, P. Müller, J. Alloys Compd., 218, 22-27 (1995).
[4] M. Schwarz, M. Haas, C. Röhr, Z. Anorg. Allg. Chem., 639, 360-374 (2013).
[5] M. Schwarz, P. Stüble, K. Köhler, C. Röhr, Z. Kristallogr., 235, 275-290 (2020).
[6] M. Schwarz, C. Röhr, Inorg. Chem., 54, 1038-1048 (2015); P. Stüble, A. Berroth, C. Röhr, Z. Naturforsch., 71b, 485-501 (2016).
We would like to thank the Deutsche Forschungsgemeinschaft for financial support.