# The first ternay sodium zincides/cadmides: Syntheses and crystal structures of Na8(Cd1-xZnx)17 (x=0.124) and Na47(Cd1-xZnx)102 (x=0.088)
## I. Junker1, K. Köhler1, C. Röhr1
### 1Institut für Anorganische und Analytische Chemie, University of Freiburg, Germany
### inga.junker@email.uni-freiburg.de
In the course of systematic studies on alkaline earth (AII) zincides/cadmides, we expanded our recent work to include the corresponding sodium phases. In contrast to the wide variety of compounds found in the system Ca-Zn-Cd [1], the number of binary Na metallides is already very limited, ternary compounds were unknown. Besides 'NaCd2', both binary sections Na-Zn and Na-Cd contain only one intermetallic compound (NaZn13, Na2Cd11). For these two Na-poor phases we determined a very small substitution of Zn Cd. Close to the complex cubic Samson phase 'NaCd2' [2], the isotypic ternary Zn-poor compound Na47Cd93Zn9 (Fd3m, a=3034.2(8) pm, R1=0.0482) and a new orthorhombic phase, Na8Cd14.9Zn2.1 (Pnma, a=972.34(3), b=1534.39(5),
c=1572.74(5) pm, Z=4, R1=0.0569) are obtained. In the structure of the latter phase [Fig. 1 (a)], most sodium atoms exhibit [NaM12] truncated tetrahedra (tt) as cation coordination polyhedra (ccps; blue/green/magenta polyhedra). In contrast to the Laves phases with mainly vertex-sharing [M4] tetrahedra inbetween the tt, the space between the ccps consists of clusters of six face-sharing [M4] tetrahedra forming icosahedra caps (light pink). The overall structure exhibits [M4], [NaM3] and [Na2M2] tetrahedra only, thus representing a further example of a tetrahedrally close packing (t.c.p., FK phase). For Na47Cd93Zn9 the small amount of Zn serves to solve mainly all problems reported for the structure refinement of the pure cadmide ’NaCd2’ [2-4] and related phases like e.g. β-Mg2Al3 (Na/Cd, Mg/Al mixed positions, partial site occupation etc.) and finally allows a reliable bandstructure calculation for these complex structures. The first of the two interpenetrating diamond-like networks [A, Fig. 1 (b)] shows a directly visible analogy to the classical Laves phases, whereas network B is commonly described using a cluster shell approach. Regardless of this different description, both substructures are again t.c.p. with tt as Na ccps (blue polyhedra) and therewith also show similar chemical bonding features [5].

###### Figure 1: Crystal structure of (a) Na8Cd14.9Zn2.1, (b) Na47Cd93Zn9 ; Zn(9)2 dumbbells, solving the disorder problem of larger Cd in the overlap region between the outer F^76_40 [Cd(5,6,7,9,11,12)] balls (blue), additionally obliterating the disorder in the F^28_16 [Na(5,6)/Zn(9)] shell (yellow).
[1] M. Wendorff, C. Röhr. Acta Cryst. A80 e218 (2024).
[2] St. Samson, Nature 4838, 259-262 (1962).
[3] Q.-B. Yang, St. Anderson, Acta Cryst. B43, 1-14 (1987), ibid. 14-16.
[4] G. Bergman, Acta Cryst. B52, 54-58 (1996).
[5] D. C. Fredrickson, St. Lee, R. Hoffmann, Angew. Chem. 119, 2005-2023 (2007).