# Magnetic Anisotropy in Layered

# Vanadyl Phosphates: Insights from DFT+U and

# X-Ray Charge Density Studies

## Lovro Šarić1, Ivica Živković2, Sergey V. Churakov1,3, Simon Grabowsky4, Lorraine A. Malaspina4, Rebecca Scatena5, Georgia Cametti1

### 1Institute of Geological Sciences, University of Bern, CH-3012 Bern, Switzerland, 2Laboratory for Quantum Magnetism, Institute of Physics, EPFL, Lausanne, CH-1015, Switzerland, 3Laboratory for Waste Management (LES), Villigen, PSI, CH-5232, Switzerland, 4Department of Chemistry, Biochemistry and Pharmacy, University of Bern, CH-3012, Bern, Switzerland, 5Diamond Light Source, Harwell Science and Innovation Campus, Didcot, OX11 0DE, United Kingdom

### Email of communicating: lovro.saric@unibe.ch

2D Layered Vanadyl Phoshates and their metal-intercalants have garnered attention through the decades due to their catalytic, optical and magnetic properties [1]. When intercalated by 3dtransition metals*,* they provide a platform to study geometrical frustration, low-dimensional magnetism and anisotropy, owing to their dimensionality. This study examines two isostructural tetragonal compounds, Ni(VO)2(PO4)2\*4H2O and Co(VO)2(PO4)2\*4H2O, space group *I4/m*. Their structure consists of V4+ square pyramids interconnected via four phosphate tetrahedra to form layers in the ab crystallographic plane, linked along the c-axis through V=O-M-O=V (M = Ni2+, Co2+) linear trimer units, with M in an MO2(OH2)4 octahedral coordination (Figure 1). This introduces an interesting through-space magnetic exchange interaction among V4+ ions in the plane whilst M interact through the oxygen ligand by magnetic superexchange.  
  
Previous studies suggest bulk ferromagnetic coupling based on an isotropic linear trimer spin Hamiltonian model, with assumed overlap of orthogonal eg d-orbitals[2]. However, inverse susceptibility plots indicate antiferromagnetic interactions. To clarify this, we combined oriented magnetic measurements on single crystals, *DFT+U* calculations, and X-ray charge density analysis.

Oriented susceptibility measurements reveal a low-dimensional, anisotropic behaviour: ferromagnetic along c, antiferromagnetic in the *ab*-plane due to a partial moment cancellation. Long-range ordering occurs at TC = 4 K, confirmed by Heat Capacity (Cp) measurements. DFT+U electronic structure calculations using *CP2K* code [3] indicate significant d-orbital overlap beyond the assumed orthogonality. X-ray charge density analysis at 100 K, employing Multipole Modelling (WINXD2024[4]) corroborates these findings, aligning with theoretical orbital populations.

Our results suggest dominant short-range spin-spin correlations, low-dimensional interactions within the *ab*-plane, preceding long-range ordering of trimers.



###### **Figure 1**. Layered structure of M(VO)2(PO4)2\*4H2O compounds, showing trimer linker motifs (upper right) and Vanadyl phosphate layers (lower right), with magnetic super-exchange interaction pathways (green and blue arrows indicating interplane and intraplane pathways respectively)

#### [1] Huang, H.-L.; Lii, K.-H.; Wang, S.-L. Really Understanding Layered Vanadyl Phosphate Hydrates. Journal of the Chinese Chemical Society 2014, 61, 199–206

#### [2] Zheng, L.-M.; Lii, K.-H. Magnetic Properties of M(VOPO4)2 · 4 H2O (M –– Co(II), Ni(II)), Layered Compounds Containing Distinct Magnetic Linear Trimers. Journal of Solid State Chemistry 1998, 137, 77–81

#### [3] Kuehne, T. D. et al. CP2K: An electronic structure and molecular dynamics software package - Quickstep: Efficient and accurate electronic structure calculations. The Journal of Chemical Physics 2020, 152, 194103.

#### [4] Volkov, A.; Macchi, P.; Farrugia, L. J.; Gatti, C.; Mallinson, P.; Richter, T.; Koritsanszky, T. XD2024 - A Computer Program Package for Multipole Refinement, Topological Analysis of Charge Densities and Evaluation of Intermolecular Energies from Experimental and Theoretical Structure Factors. 2024.